## Slide 1
Multi-scale characterization of hydrogels of biological interest
Supervisors:
FAST : Frédérique GIORGIUTTI – Ludovic PAUCHARD
CEA : Patrick GUENOUN – Jean-Philippe RENAULT
Souhaila N’MAR – 3rd year PhD Student
Cryo-SEM of hydrogel
Deformation of colloidal gel

## Slide 2
Context
Food industry
Du et al (2021)
Agriculture
Sabbagh et al. (2019)
Hydrogel
Drug delivery
Cluff et al. (2014)
Besarab (2021)
Hydrogel 3D structure

## Slide 3: Context
1
Objective
Develop hybrids hydrogels based on nanoparticles and macromolecules (proteins).
Bovine serum albumin
2
3
How ?
Macroscopic scale
Microscopic scale
Why ?
200 nm
Nanoindentation
Dry gel
Swollen gel
Imbibition
Biomedical applications (drug delivery)
Main goal:
Link between structure and mechanical properties of the gel
SAXS
Rheology
Cryo-TEM/SEM
Silica
nanoparticles
Silica
+
ionic species
(NaCl)

## Slide 4
Two types of gels
Silica NP
LUDOX TM50 =22
=15%
pH=9
Charge : Negative
Silica NP
Hydrogel (onlyNP) - Silica + ionic species (NaCl)
Biohydrogel (NP+protein)
Silica / ionic species / BSA
System:
(A) Structure of
protein : Bovine Serum Albumin (BSA)
DLVO theory
I=Ionic strength=[
(B) Distribution of charge of BSA
positive-blue
negative-red
neutral-white
At pH=7 , BSA is globaly negatively charged
*NP=nanoparticle
44 nm
Without ionic species
With ionic species

## Slide 5: Macroscopic characterization : Phase diagram (OnlyNP)
G
Drying time
Accumulation of particles at the surface of the drop
Skin formation time
R

## Slide 6: Macroscopic characterization : Phase diagram (OnlyNP)
Crack
Buckling
R
N’MAR et al. , Soft Matter , 2023

## Slide 7: Before gelation ? Rheology
Hydrogel (onlyNP)
Variation of the elastic modulus with the concentration of BSA

## Slide 8: Microscopic characterization : Mixture of Silica and BSA
Depletion process
CryoTEM images
SAXS measurements
Silica + BSA dispersion
SAXS measurements
Silica dispersion

## Slide 9: Microscopic characterization : SAXS measurements - Gels
« Biohydrogel porosity
is lower than
the hydrogel »
Attractive potential
CryoSEM images
Porod
Size of cluster

## Slide 10: Link between structure and mechanical properties of the gel
Well depth = energy of interactions
2R(λ-1) = range of interactions=width of the square well
Attractive potential
Intersection model
ζ= agregate size
Avec
dim = euclidean dimension
[1, 2]
Weak-link regime
Strong-link regime
Phi-power-law models:
Shih et al (1990)

## Slide 11: Perspectives / Study of imbibition of sessile drops and release of BSA protein
release of BSA
Imbibition – swelling and apparition of
mechanical instabilities
Crack

## Slide 12: Thank you for your attention

## Slide 13
Thank’s to:
Frédérique GIORGIUTTI
Ludovic PAUCHARD
Patrick GUENOUN
Jean-Philippe RENAULT
Thomas GIBAUD
Frédéric GOBEAUX
François Boulogne
Alain CARVALHO
Raphaël PIDOUX
Javier PEREZ
Soleil Synchrotron
FAST Laboratory
More details available in :
Souhaila N’Mar et al. ; Structuration and deformation of colloidal hydrogels. Soft Matter, 2023.