## Slide 1
ANTHONY VARLET
Thesis Director: Philippe Brunet
Co-director: Laurent Limat
Supervisor: Julien Dervaux
Co-supervisor: Matthieu Roché
Delayed coating of a liquid film on a deformable substrate, in a partially wetted condition

## Slide 2
Introduction : Wetting statics
: Surface energy between phases i and j (J/m²)
: contact angle (°) (at equilibrium)
Red dot: contact line

## Slide 3
Introduction : Wetting dynamics
→ forward contact angle (°)
→ backward contact angle (°)
Ph.D. of M. Oléron, 2022
Above a critical droplet speed
→ liquid deposition regime
Drop in movement → induces viscous stress
→ : Capillary number

## Slide 4
Context of this study
Rigid
Soft
Deformation at contact line → Additional dissipation →What changes?
Substrate deformation → Favors or damps instabilities at contact line?
Questions

## Slide 5
Experimental set-up
2 classic set-ups:
Sliding droplet
Dip-coating
Straight contact line
Pulling speed: controlable parameter
Sylgard 184™ Elastomeric Gel (Dow Corning)
→ Young modulus : 7 kPa – 1,6 MPa *
* Glover, J. D. et al, 2020 JOURNAL OF POLYMER SCIENCE
Liquid used : Pure Glyverol ()

## Slide 6
Dip-coating : Non-deformable case
Total wetting
Partial wetting
Criteria of coating
Trapezoidal shape
Contact line on the side receding during extraction
Bulge near the contact line
Separate edge of contact line with rest of the film (LLD-like)
Uniform thickness
Landau-Levich-Derjaguin*:
For any
T. D. & Ruschak, K. J., 1979 Nature
Snoeijier, J. et al., 2006 PRL
*L. D. Landau and B. V. Levich, 1942 Acta Physicochim.

## Slide 7
Observation with deformable substrate
Coating not instantaneous, unlike rigid case
→Delay of liquid entrainment
Lower Young Modulus shifts the range toward lower
Sharp decrease of τ with
Origin?
Support
PDMS
Contact line
1 mm
V
PVC
Coating with treshold in , like rigid case

## Slide 8
Phenomenom 1 : Slowly deforming surface of substrate
Force balance at contact line:
Horizontal: balance of capillary forces and viscous shear stress
Vertical: elasticity of substrate counterbalances capillary force
Deformation at contact line
Elastocapillary length:
More (slowly increasing) dissipation
Contact line in movement → Propagating ridge
Slow & progressive growth of the ridge
Inside the solid
S.J. Park et al., 2014 Nature

## Slide 9
Phenomenom 2 : Free-chains slowly moving toward the surface
Red chain
Blue chain
Yellow chain « Free-chain »
Free-chain washing
Entrainement delay should be suppressed
During extraction
Close to the contact line
Slow reorganization of free-chains
Poroelasticity
Polymer network
Ph.D. of M. Oléron, 2022

## Slide 10
Conclusion
Unlike rigid case: delay for liquid entrainment
delay time decreases strongly with
Possible mechanisms underlying delay:
  presence of free-chains in substrate Work in progress
  substrate deformability Smaller range of for a smaller Young’s modulus
  favor liquid entrainment?

## Slide 11
Thanks everyone for your attention !!!

## Slide 12
Introduction : Context of this work
Above a critical droplet speed→ liquid deposit regime
Characterize this regime with θ
In theory
In practice
(near 30°)
Change experimental system
→ study contact line with simpler geometry
Contradiction with the experiment not well understood
→ back of a drop not fully understood
α
*Ph.D. of M. Oléron, 2022
*

## Slide 13
Origin 1 : Deformable surface
Force balance at contact line:
Horizontal: balance of capillary forces ()
Vertical: elasticity of substrate meet capillary force
Deformation at contact line
Elastocapillary length:
Rigid
Deformation
Soft
Can impact the flow
Slow & progressive growth of the ridge at contact line in movement
S.J. Park et al., 2014 Nature
[Thickness film ~ 10-100 µm]

## Slide 14
Dip-coating : Non-deformable case
Total wetting
Partial wetting
Criteria of coating
Viscous dissipation
Trapezoidal shape
Contact line on the side receding during extraction
Bump at contact line
Separate edge of contact line with rest of the film (LLD-like)
Uniform thickness
Landau-Levich-Derjaguin:
For any Ca
T. D. & Ruschak, K. J., 1979 Nature
Snoeijier, J. et al., 2006 PRL

## Slide 15
Sample used : PDMS (polydimethyl-siloxane) used:
Sylgard 527™ Dielectric Gel (Dow Corning) → Young’s modulus : 3 kPa
Sylgard 184™ Elastomeric Gel (Dow Corning) → Young’s modulus : 7 kPa – 1,6 MPa
Liquid used :
Glycerol (more & less) pure, G100 :
,
Ucon (lubricant, Dow Corning) :
,
Properties of sample & liquid used

## Slide 16
Liquid in movement
Viscous energy dissipation in the liquid
Propagation of the deformation
→ Energy dissipation in solids of viscoelastic origin
Importance of viscoelastic energy dissipation: relaxation ratio 𝑅
, most of the energy dissipated in the solid state
, equivalent energy dissipation in solids and liquids
, energy dissipation exclusively in the liquid
Dissipation ratio

## Slide 17
Phenomenom 2 : Free-chains slowly moving toward the surface
Red chain
Under stress: stretch and store elastic energy
Blue chain
Yellow chain « Free-chain »
Under stress: can relax and/or move in the network
mechanical response with viscoelastic contribution
Free-chain washing
Entrainement delay should be suppressed
During extraction
Close to the contact line
Slow reorganization of free-chains
Poroelasticity
Polymer network
Ph.D. of M. Oléron, 2022

## Slide 18
Phenomenom 1 : Slowly deforming surface of substrate
Force balance at contact line:
Horizontal: balance of capillary forces and viscous shear stress
Vertical: elasticity of substrate compete capillary force
Deformation at contact line
Elastocapillary length:
More (slowly increasing) dissipation
Contact line in movement → Propagating ridge
Slow & progressive growth of the ridge
Inside the solid

## Slide 19
Time condition
Transition time : time between of dip velocity to pulling velocity
In experiment : 200-500 ms
Augment this time Influence?
Waiting time between diping
Substrate as a time to come-back to is initial state
Influence the coating Have an « history »
Video 2 – Time between dip : 30 secondes.
Left : n°1, middle : n°3, right : n°5.
How many secondes waiting?
Experiment at fixed Ca and compared coating delayed for 30, 100 and 1000 secondes

## Slide 20
Observation with deformable surfaces
Coating not instantaneous, unlike rigid case
→Delay at liquid entrainment
Possible master curve guiding the delay time with
Origin?
Support
PVC
PDMS
Contact line
1 mm
V

## Slide 21
Origin 1 : Young modulus effect
Sylgard 184 :
1,6 Mpa → Shift lower Ca for delay (~)
845 kPa → Shift less lower Ca for delay (~)
Same results with lower Young’s modulus (7, 59, 245 & 845 kPa) ?
Less free chain in Sylgard 184
add free-chain ?

## Slide 22
Introduction : Context of this study
In theory
In practice
(near 30°)
Change experimental system
→ study contact line with simpler geometry
Contradiction with the experiment not well understood
→ back of a drop not fully understood

## Slide 23
Time condition : Sylgard 527 (3 kPa)
Figure 11 – Waiting time for Sylgard 527 between dipping of the substrate at Ca = 4 10-2 .
Left : Wait time = 30s. Middle : 100s. Rigth : 1000s.
Sylgard 527 → not reliable enough

## Slide 24
Time condition : Sylgard 184 (1,6 MPa)
Figure 12 – Waiting time for Sylgard 184 between dipping of the substrate at Ca = 4 10-2 .
Left : Wait time = 30s. Middle : 100s. Rigth : 1000s.
Sylgard 184 at 1,6 MPa → wait time of 100s sufficient reliable

## Slide 25
Time condition : Sylgard 184 (7 kPa)
Figure 13 – Waiting time for Sylgard 184 between dipping of the substrate at Ca = 9,4 10-5 .
Left : Wait time = 100s. Rigth : 1000s.
Sylgard 184 at 7 kPa → Hard to define wich waiting time

## Slide 26
Perspectives : Shape of contact line
Figure 12 – Shape of contact line.
Sample’s width : 30,25 mm
Figure 13 – Shape of contact line.
Sample’s width : 69 mm
Instability-like?
Average « wavelength » of ondulation?
Size dependent?
Upgrade program & ligthing of set-up

## Slide 27
Introduction : Context of this work
From a critical droplet speed
→ liquid deposit regime
Same in rigid case
Characterize this regime as a function of the contact angle
Theoretically
(rigid and soft)
In practice
(rigid and soft)
(near 30°)
Need to change experimental system to study contact line with simpler geometry
Contradiction with the experiment not well understood because the back of a drop not fully understood
Figure 2 - Shape of droplet in function of Bond number (PHD of M. Oléron, 2022).
The images framed in red are for the case of a rigid (T. Podgorski et al., PRL 2001)

## Slide 28
Origin 2 : Presence of free-chain in the substrate
Red chain
Under stress:
stretch and store elastic energy
Blue chain
Yellow chain
« Free-chain »
Under stress: can relax and/or move in the network
mechanical response with viscoelastic contribution
1 lead for delayed coating:
slow reorganization of free chains near the contact line during extraction
Free-chain extract
If coating instantaneous

## Slide 29
Experimental set-up
Figure 3 – Experimental set-up : dip-coating
Sample used : PDMS (polydimethyl-siloxane) used:
Sylgard 527™ Dielectric Gel (Dow Corning) → Young’s modulus : 3 kPa
Sylgard 184™ Elastomeric Gel (Dow Corning) → Young’s modulus : 7 kPa – 1,6 MPa
Liquid used :
Glycerol (more & less) pure, G100 :
,
Ucon (lubricant, Dow Corning) :
,
Straight contact line
Pulling speed : controlable parameter
2 classical set-up :
Sliding droplet
Dip-coating
α