## Slide 1: Interaction ion-ion véhiculée par la contrainte dans les cristaux dopés aux ions de terres rares
Anne Louchet-Chauvet, Thierry Chanelière
Congrès SFP 2023, 3-7 juillet 2023

## Slide 2
Quantum technologies and decoherence
Atomic two-level system in a superposition state
Quantum storage /
Quantum repeaters
Quantum bits /
Quantum computation
Quantum sensors
Quantum conversion
Quantum optomechanics
Decoherence!

## Slide 3
Quantum technologies and decoherence
Atomic two-level system in a superposition state
Quantum storage /
Quantum repeaters
Quantum bits /
Quantum computation
Quantum sensors
Quantum conversion
Decoherence!
Quantum optomechanics
5
Optical ()
Spin ()
At :
Exceptionally
narrow lines
Rare-earth ion-doped crystals:
Ultra-coherent solid-state quantum systems

## Slide 4
Quantum technologies and decoherence
Atomic two-level system in a superposition state
Quantum storage /
Quantum repeaters
Quantum bits /
Quantum computation
Quantum sensors
Quantum conversion
Quantum optomechanics
Intrinsic decoherence
 homogeneous width
Non-stationary environment
 spectral diffusion
Decoherence!

## Slide 5
Environment-induced decoherence
Example #1: magnetic noise induced spectral diffusion
    If Zeeman sensitivity  Spectral diffusion
Example #2: Electric noise induced spectral diffusion
Random, spontaneous spin flips
in the vicinity of the quantum system
 Magnetic field noise
Random, spontaneous movements of electric dipoles or charges in the vicinity of the quantum system
 Electric field noise
    If Stark sensitivity  Spectral diffusion

## Slide 6
Environment-induced decoherence
Example #3: Acoustic noise (in condensed matter systems)
Time-dependent strain
    If stress sensitivity  Spectral diffusion
Absorption
Frequency
Piezospectroscopic effect
Lineshift
Stress
Interatomic distances change
Modifies the local crystal field
Hooke’s law

## Slide 7
Excitation-induced decoherence
2 atoms at close distance
Electric dipole
moment change
+ Stark effect
Magnetic dipole moment (spin) change
+ Zeeman effect
Excitation-induced strain
+ piezospectroscopic effect
Ion-ion
interaction
Magnetic
dipole-dipole
interaction
Electric
dipole-dipole
interaction

## Slide 8
Excitation-induced strain
Outer atomic size depends on
electronic configuration (orbitals)
Piezo-excitonic backaction in embedded quantum dots
J. Kettler et al. Nature nanotechnology, 16(3), 283-287 (2021)
A. Louchet-Chauvet et al., arXiv:2109.06577 (2021).
Piezo-orbital backaction in
rare-earth ion-doped crystals
Stress
Optical excitation
Strain in crystal
Electronic orbital shape change
Hooke’s law

## Slide 9
Stress
Optical excitation
Strain in crystal
Piezo-orbital backaction
Electronic orbital shape change
Excitation-induced strain + piezospectroscopic effect
in rare-earth ion-doped crystals
Hooke’s
law
Line shift
Interatomic distances change
Modifies the local crystal field
Piezospectroscopic effect
Hooke’s law
Keating, K. B. et al. (1961) Effect of pressure on the spectra of rare earth ions in crystals. The Journal of Chemical Physics, 34(1), 143-151.

## Slide 10
Excitation-induced decoherence
2 atoms at close distance
Electric dipole
moment change
+ Stark effect
Magnetic dipole moment (spin) change
+ Zeeman effect
Excitation-induced strain
+ piezospectroscopic effect
Ion-ion
interaction
Strain-mediated
ion-ion interaction
Magnetic
dipole-dipole
interaction
Electric
dipole-dipole
interaction

## Slide 11
Ion-ion interactions in RE-doped crystals
Three different ion-ion interactions with similar scaling law:
Electric dipole-dipole interaction
Magnetic dipole-dipole interaction
Strain-mediated interaction
Ion with electronic
or nuclear spin
(Kramers/non-Kramers)
Expected
variability for

## Slide 12
Ion-ion interactions in RE-doped crystals
Three different ion-ion interactions with similar scaling law:
Electric dipole-dipole interaction
Magnetic dipole-dipole interaction
Strain-mediated interaction
Ion with electronic
or nuclear spin
(Kramers/non-Kramers)
Site symmetry allowing permanent dipole moment
Expected
variability for

## Slide 13
Expected
variability for
Ion-ion interactions in RE-doped crystals
Three different ion-ion interactions with similar scaling law:
Electric dipole-dipole interaction
Magnetic dipole-dipole interaction
Strain-mediated interaction
Ion with electronic
or nuclear spin
(Kramers/non-Kramers)
Mechanical characteristics
of crystal
Site symmetry allowing permanent dipole moment

## Slide 14
Expected
variability for
Ion-ion interactions in RE-doped crystals
Three different ion-ion interactions with similar scaling law:
Electric dipole-dipole interaction
Magnetic dipole-dipole interaction
Strain-mediated interaction
Ion with electronic
or nuclear spin
(Kramers/non-Kramers)
Mechanical characteristics
of crystal
Site symmetry allowing permanent dipole moment

## Slide 15: Comparing ion-ion interactions in RE-doped materials
10 orders of magnitude!
Strain-mediated
ion-ion interaction
Magnetic
dipole-dipole
interaction
Electric
dipole-dipole
interaction
Experimental measurements via excitation-induced decoherence
Excitation-induced decoherence in atomic ensembles:
Usually explained with only magnetic and electric dipole-dipole interactions
 Mostly works !
Including the strain-mediated contribution
 better understanding
… in 10 rare-earth-doped compounds
except in high-symmetry, low spin compounds

## Slide 16: Conclusion
Excitation-induced decoherence in rare-earth ion-doped crystals
3 different mechanisms with same spatial scaling:
 magnetic dipole-dipole interaction
 electric dipole dipole interaction
 strain-mediated interaction (never negligible!)
Ion-ion
interaction
Quantum storage /
Quantum repeaters
Quantum bits /
Quantum computation
Quantum sensors
Quantum conversion
Quantum optomechanics
A. Louchet-Chauvet, T. Chanelière, Strain-mediated ion-ion interaction in rare-earth-doped solids. Journal of Physics: Condensed Matter 35, 305501 (2023)

## Slide 17: Perspectives
A. Louchet-Chauvet, T. Chanelière, Strain-mediated ion-ion interaction in rare-earth-doped solids. Journal of Physics: Condensed Matter 35, 305501 (2023)
Ion-ion interactions
Ion-ion
interaction
Strain-coupling
Mechanical degree of freedom
Quantum
degree of freedom
Interesting perspectives in hybrid optomechanics
Source of decoherence
Building block for quantum computing
Compounds where only the strain-mediated ion-ion interaction dominates
 Pure ion-ion interaction mechanism
Piezo-orbital backaction
Piezospectroscopic effect

## Slide 18: Acknowledgments
Loïc Morvan
Perrine Berger Sacha Welinski
Lothaire Ulrich
Yoann Attal
François Ramaz
Xiaoping Jia
Thomas Llauze
Félix Montjovet
Alban Ferrier
Philippe Goldner
Thierry Chanelière
Jean-Philippe Poizat
Rose Ahlefeldt
Julian Dajczgewand
Jean-Louis Le Gouët
Lucile Veissier
Thibault Courageux
Hans Lignier
Pierre Verlot
Ludovic Bellon

## Slide 19: Cryogenic or room temperature ?
: crystalline matrix defects and disorder
 insensitive to temperature
: dynamic processes (phonons)
Absorption
Frequency
All ions identical!
Ions not identical
 Selection of a ion subset with SHB
Absorption
Frequency
Collective enhancement

## Slide 20: Modeling the piezo-orbital backaction
Pump
beam spot
Surface
displacement
Time ()
Atomic population evolution in the whole crystal volume
Corresponding volumic change assuming simple ionic radius change
Propagate strain towards the surface
Calculate the surface displacement
Derive the corresponding deflection angle

## Slide 21: Modeling the resonant photothermal backaction
Pump
beam spot
Surface
displacement
Calculate the time-dependent phonon heatload in the whole crystal volume

## Slide 22: Modeling the resonant photothermal backaction
Resonant photothermal effect:
Very well known in RE-doped crystals!
(including at room temperature)
Wavenumber ()

## Slide 23: Modeling the resonant photothermal backaction
Resonant photothermal effect:
Very well known in RE-doped crystals!
(including at room temperature)
Energy levels and relaxation rates ()
for room-temperature Tm:YAG
Caird, J. et al., (1975). Characteristics of room-temperature 2.3-µm laser emission from Tm3+ in YAG and YAlO3. IEEE Journal of Quantum Electronics, 11(11), 874-881.
Wavenumber ()
Tm-Tm cross relaxation
Radiative relaxation
(fluorescence)
Non-radiative relaxation
(phonons)
Rate equations for this 4-level system
 Time-dependent phonon rate generation (heatload)

## Slide 24: Modeling the resonant photothermal backaction
Pump
beam spot
Surface
displacement
Calculate the time-dependent phonon heatload in the whole crystal volume
Feed heatload in heat equation to derive temperature in the whole crystal volume
Corresponding volumic change using thermal expansion coefficient for YAG
Propagate strain towards the surface
Calculate the surface displacement
Derive the corresponding deflection angle

## Slide 25: Model results
Piezo-orbital backaction
Photothermal backaction
Time evolution:
given by atomic populations in
(instantaneous effect)
Spatial shape:
narrow bump with constant width
Time evolution:
Instantaneous at center
Delayed at a distance
Spatial shape:
progressive broadening (heat diffusion)

## Slide 26: Optomechanical backaction in a rare-earth ion-doped crystal
Demonstration in a bulk sample, enabling time- and space-resolved tomography
Both effects are connected to atomic internal dynamics
No parasitic photothermal contribution
A dissipative, photothermal effect
(phonons generated throughout relaxation)
A conservative, piezo-orbital effect
(geometric shape of the electronic orbitals)
Louchet-Chauvet, A. et al. (2021). Optomechanical backaction processes in a bulk rare-earth doped crystal. arXiv preprint arXiv:2109.06577.

## Slide 27: Challenges of observing piezo-orbital backaction
Collective enhancement with a large number of identical ions
Very small
piezo-orbital effect!
Typical relative ionic radius change upon excitation:
(
Bulk object:
Large number of atoms / quantum systems (limited by beam size)
No mechanical resonance
  weak response but time-resolved study
Usually in optomechanics: Mechanical resonator
Sharp mechanical resonance
 large response
Low number of atoms / quantum systems
Pump
beam spot
Surface
displacement
  Room temperature:
  All ions identical

## Slide 28: Which quantum system / ion ?
Wavenumber ()
Energy levels and transitions for
of ions in level after
resonant excitation
identical ions in laser beam transferred to a different electronic state
Goal: long-lived energy levels
to maximize the population transfer
Enhancement factor
Incoherent optical pumping for

## Slide 29: Excitation-induced motion in a bulk Tm:YAG crystal
(c)
Close to bump center
Further away
Is it really a piezo-orbital signal ?
 Photothermal contribution !? 
deflection
Time evolution resembles the evolution
Attenuated deflection
!!! Delayed actuation !!!

## Slide 30: Elucidating the optomechanical processes 1) resonant nature ?
Scan the pumping laser wavelength around
Wavenumber ()
Many transitions between Stark multiplets
Deflection signal is resonant!
Resonant piezo-orbital backaction?
Resonant photothermal backaction?

## Slide 31: Elucidating the optomechanical processes 2) spatio-temporal dynamics ?
Bulk crystal
 Time-resolved measurements
 Spatially-resolved measurements!
Resonant piezo-orbital backaction
Resonant photothermal backaction
?
Model both piezo-orbital and photothermal effects
  (in time and space)

## Slide 32: Resonant photothermal effect model
Energy levels and relaxation rates ()
for room-temperature
Caird, J. et al., (1975). IEEE Journal of Quantum Electronics, 11(11), 874-881.
Wavenumber ()
Tm-Tm cross relaxation
Radiative relaxation
(fluorescence)
Non-radiative relaxation
(phonons)
Population dynamics and relaxation processes
Calculate phonon heatload over time
    Heat diffusion equation
 Temperature distribution
Linear thermal expansion ()
 photothermal surface displacement
 photothermal deflection angle

## Slide 33: Model vs experimental data
Fit to the experimental data
Piezo-orbital part with
time evolution imposed by
Photothermal part
fully imposed by model
Excellent agreement with data
Piezo-orbital part:
Lorentzian bump with height
at its maximum
Overall force to distort the surface :
()
A. Louchet-Chauvet, P. Verlot, J.-P. Poizat and T. Chanelière, arXiv:2109.06577 (2021).
(compare 50aN/quantum dot)
J. Kettler et al. Nature nanotechnology, 16(3), 283-287 (2021)