## Slide 1
Mathieu Lizée
Ecole Normale Supérieure de Paris
Dynamical couplings at the liquid-solid interface

## Slide 2: Nanofluidics, everywhere
From biological ion machinery…
… to large-scale membranes
for desalination and energy harvesting.
…to artificial nanochannels…

## Slide 3: Dynamical couplings at the liquid solid interface
For long, the liquid solid interface has remained a static problem
Double layer capacitance, Stern layer…
Secchi, Nature 2016
Kavokine et al, Nature 2022
Yu, Bonn, Kavokine et al, Nature Nano 2023
These dynamical couplings rely on the interplay between liquid and solid excitation spectrum
Coupling with water can even cool down electrons !
Carbon nanotube friction is controlled by interlayer graphite plasmon

## Slide 4: New effects at the liquid solid interface
In nanoscale hydrodynamics, excitation spectrum of the solid state matters
Liquid slip
Electron flow ?
Liquid flow
Electron cooling

## Slide 5: Current generation mechanisms
Coulomb drag
Rabinowitz et al, Nano Letter 2020
Chen et al, Nano Letter 2023
Capacitive charging
Yin et al, Nature Nano 2014
Water + Salt droplet moving on graphene surface
Phonon drag ?
Kral & Shapiro, PRL 2001

## Slide 6: Micrometric flow on graphene transistor
50 𝜇m
Viscous liquid
Graphene transistor as flow sensor
Homemade AFM deposits a small droplet
Solid
Alice Marcotte

## Slide 7: Let us move the droplet
Droplet motion induces current in the flake
A

## Slide 8: Roughness controls the generated current
Generated current depends on position and direction…
(Cartoon)
…because of the random orientation of wrinkles.
- Instrumental role of corrugations
- Nature of liquid is not relevant
Driving mechanism is viscous friction and not a moving potential or charge adsorption-desorption
3 liquids : apolar, polar, ionic
Glycerol, Ionic liquid and silicon oil
All yield similar current

## Slide 9: Tuning electronic properties ?
Graphene is one of the rare materials where charge carrier density is easily tunable
Generated current is proportional to bias but also measured at zero bias

## Slide 10: A unified picture of liquid-solid interface dynamics
Out of equilibrium perturbation theory in the Keldysh formalism
Electronic propagator
Bosonic propagator
…
Coquinot et al, PRX 2023
This formalism allows to write on the fame footing phonon and electron transfer
Fully unified picture of dynamics at liquid-solid interfaces
Heat Transfer, Friction, Current generation…
Baptiste Coquinot

## Slide 11: Phonon wind blows on Fermi sea
Fermi Sea
Bosonic wind
Electrode probes current
Phonon wind
dominates
- Instrumental role of corrugations
- Nature of liquid is not relevant

## Slide 12: Quantitative agreement !
Electronic distribution :
Phonon wind velocity computed using momentum balance
Comparison with experiment : is the non-dimensional corrugation
Electronic current :
Band structure
We model graphite as a 2DEG
Friction induced current mediated by phonon wind

## Slide 13: Negative quantum friction
Quantum feedback
When phonon drag dominates, can overtake
electrons will give back momentum to the liquid
if the solid is unable to relax momentum,
then all momentum is given back to liquid
Huge reduction of friction
Coquinot et al, PRX 2023

## Slide 14: New paradigm : liquid-solid coupling
We probe a phonon wind mediated electric current
Very peculiar setup :
High viscosity, small droplet, 2d material, wrinkles
We predict a reduction of friction by metallic electrons

## Slide 15
Phonon drag current (experiment)
Lizée & Marcotte et al, PRX 2023
Quantum feedbacks (theory)
Coquinot et al, PRX 2023
Follow-up here :

## Slide 16: Solid-liquid friction
No slip
Partial slip
Slip length
Slippage is very important in nanoscale channels!

## Slide 17: Quantum friction
Kavokine et al, Nature 2022
Electronic properties of the solid walls influence friction
Small radius
Large radius
Misaligned layers Graphene like
Aligned layers Graphite like wall
Surface plasmons, Phonons
Liquid
Hydron
Solid
Coulomb interaction
The stronger the quasiparticle overlap, the stronger the friction
Interlayer plasmon in graphite
stronger friction than on graphene
« Quantum friction » due to electronic fluctuations coupled to water
Secchi et al, Nature 2016