## Slide 1: Physique des décharges capacitives radiofréquence
Pascal Chabert
Laboratoire de Physique des Plasmas
Ecole Polytechnique, France
Congrès Général de la Société Française de Physique, 2023

## Slide 2: RF Plasmas in industry
Plasma
P = 0.1-10 Pa
+
+
+
+
+
e-
Cl
Si
SiCly
Clx+
Cl
Cl
Cl
Cl
Plasma etching
Plasma deposition

## Slide 3: Industrial Challenges for RF Plasmas
Patern size shrinks while substrate size increases
Need stability, reproductibility and uniformity
m-electronics
LCD - Flat Panel Displays

## Slide 4
Capacitive discharges
Inductive discharge

## Slide 5: Energies and densities

## Slide 6: Dispersion relation of EM waves
Non-magnetized plasmas behave like conductors at low frequency and like dielectrics at high frequency

## Slide 7: Electrodynamics in the RF domain
EM waves are evanescent (without B field); they penetrate deeper than electrostatic fields
Electrons follow the RF field
Ions do NOT follow the RF field

## Slide 8: The radiofrequency sheath

## Slide 9: Electron dynamics: the homogeneous (matrix) sheath
Sheath motion non-linear with voltage
Assumes electrons follow the rf field
Assume frozen ions

## Slide 10: Voltage drive: voltage and current waveforms
Sheath response is non-linear
Sinusoidal voltage drive
Non-linear current waveform
Small contribution of the
conduction current

## Slide 11: Conduction current balance
Self bias formation

## Slide 12: Ion dynamics in the sheath
Low frequency
High frequency

## Slide 13: Resulting « bi-modal » energy distribution

## Slide 14: Capacitive discharges at low pressure

## Slide 15: Circuit model of capacitive discharges
Plasma
Vrf
Time-averaged potential
Zsheath=1/(jcsw)
Zplasma=Rp+jLpw
Impedance depends on :
Voltage, Vrf
Electron density, ne
Sheath size, sm
To find a self-consistent solution:
Child law
Particle balance
Power balance
sb(t)
sa(t)
Ez
Ez

## Slide 16: Collisionless power absorption
Rp
Rstoc
Collisionless power dissipation in the sheath
Two approaches:
Kinetic model « Hard wall »
(Fermi stochastic acceleration)
M.A. Lieberman, IEEE Plasma Sci. 16 (1988) 638
I.D. Kaganovich, Phys. Rev. Lett. 89 (2002) 265006
Fluid model « pressure heating »
G. Gozadinos et al., Phys. Rev. Lett. 87 (2001) 135004
Importance of sheath dynamics
Equivalence of the hard-wall and kinetic-fluid models of collisionless electron heating in capacitively coupled discharges T Lafleur, P Chabert, M M Turner and J P Booth Plasma Sources Sci. Technol. 23 (2014) 015016

## Slide 17
The potential in the plasma is always higher than (or equal to) the potential of the two electrodes
Potential profile in single frequency symetric discharges

## Slide 18: Potential profile in single frequency assymetric discharges
Within the homogeneous model :
The larger voltage across the smaller electrode
A DC self-bias develops:

## Slide 19: Dual Frequency with well separated frequencies
■●▲ : Experiments
----- : model
HF drive for high flux
LF bias for tunable ion energy
Dual Frequency Capacitive (DFC)
Vrf
A. Perret et al., Appl. Phys. Lett 86 ( 2005) 021501

## Slide 20: Dual frequency sheath
M. A. Lieberman, IEEE Trans. Plasma Sci. 16, 638 (1988)
J. Robiche et al, J. Phys. D. 36 (2003) 1810

## Slide 21: Indepenedent control not achieved

## Slide 22: Ion energy distribution
15 mTorr
i = 2 mm
Analyzer :
L = 1 mm
81.36 MHz
sm = 1.2 mm
13.56 MHz
sm = 7 mm

## Slide 23: Electrical assymmetry effect in dual-frequency symmetrical discharges
It is possible to change the self-bias by changing the phase between the two frequencies, even when geometrically symmetrical
The asymmetry is generated by the voltage waveform
B. G Heil, U. Czarnetzki, RP Brinkmann and T.Mussenbrock, J. Phys. D: Appl. Phys. 41 (2008) 165202

## Slide 24: Complex waveforms
This is a generalization to complex waveforms
Electron heating is also affected
T. Lafleur, P.A. Delattre, E.V. Johnson, and J.P. Booth, Appl. Phys. Lett. 101 (2012) 124104

## Slide 25: Capacitive discharges at Very High Frequency

## Slide 26: The electromagnetic regime
~
z
r
0
R
Solve Maxwell’s equations for given s and ne (not self-consistent):
  R : Standing wave effect (Ez)
  d : Skin effect (Er)
Edge effects
Hf
Ez
Er
M.A. Lieberman et al., Plasma Sources Sci. Technol. 11 (2002) 283
L. Sansonnens et al., Plasma Sources Sci. Technol. 15 (2006) 302
P. Chabert, J Phys D, 40 (2007) R63 (Review article)

## Slide 27: Transmission line model
z
0
r
dr
TL elements depends on:
Local voltage and/or current (Vrf, Irf)
Electron density, ne
Sheath size, sm
Use:
Child law
Particle balance
Power balance
Self-consistent solutions for:
Vrf (r) and Irf (r)
ne(r)
sm(r)
C’
R’cap
2R’i
L’
R’ind
dr
P. Chabert et al., Physics of Plasmas 11 (2004) 1775
P. Chabert et al., Physics of Plasmas 11 (2004) 4081
P. Chabert et al., Phys. Rev. Lett. 95 (2005) 205001

## Slide 28: Experiments
Top-grounded electrode
64 planar probes
Cartography of the ion flux
3 RFEA
Retarding Field Energy Analyser
Ion energy uniformity

## Slide 29: The standing wave effect
13.56 MHz
Ji max = 0.07 mA.cm-2
50 W, 200 mTorr (local heating)
Ji/Jimax
Ji/Jimax
Ji/Jimax
60 MHz
Ji max = 0.15 mA.cm-2
81.36 MHz
Ji max = 0.17 mA.cm-2
A. Perret et al., Appl. Phys. Lett 83 ( 2003) 243

## Slide 30: The standing wave effect
-20
-10
0
10
20
0,00
0,02
0,04
0,06
0,08
0,10
0,12
0,14
0,16
0,18
Experiments
J
i
(mA.cm
-2
)
X (cm)
TL Theory
81.36 MHz
200 mTorr (local heating)
50 W
Worsening factor
Fairly insensitive to the gas composition
P. Chabert et al., Physics of Plasmas 11 (2004) 1775

## Slide 31: Cancel the standing wave effect: the lens concept
L. Sansonnens and J.P.M. Schmitt, Applied Phys. Lett. 82 (2003) 182:
The electrode must have a Gaussian shape (in vacuum, from a solution of Maxwell’s equations)
Electrode
Electrode
Substrate
Vacuum or dielectric
Plasma
rf

## Slide 32: Capacitive discharges at high pressure

## Slide 33: Intermediate pressure: non-uniform ionization
Low-pressure transport and power disspation theories are not correct
The electron temperature is strongly non uniform due to strong energy dissipation by collisions
Ionization is strongly localized
Plasma density profiles are strongly affected
T. Lafleur and P. Chabert Plasma Sources Sci. Technol. 24 (2015) 025017

## Slide 34: Intermediate pressure: “passive bulk”
Active-sheath and passive-bulk models
Strong power absorption and dissipation in the bulk
But NO ionization because the high energy tail of eedf is strongly depleted
Strong electron heat flux from the sheath towards the bulk
E. Kawamura et al. J. Vac. Sci. Technol. A 38(2) 2020

## Slide 35: Intermediate pressure: g mode
New theories needed for EM regime with g electrons
When the pressure increases there is a sheath breakdown phenomenon when secondary electron emission is present
This well known transition is potentially unstable for large area – high frequency CCP’s
Primary e-
Positive ion
Secondary e-
Photon
Metastable
E. Kawamura et al. J. Vac. Sci. Technol. A 38(2) 2020
Emi Kawamura, Michael A Lieberman, Allan J Lichtenberg and Pascal Chabert Plasma Sources Sci. Technol. 30 (2021) 035001
M A Lieberman, E. Kawamura and P. Chabert Plasma Sources Sci. Technol. 31 (2022) 114007

## Slide 36: Atmospheric pressure CCP’s
The RF field does penetrate the plasma because of nearly dielectric limit
The electron temperature oscillates in time during an RF cycle because of very fast energy relaxation by collisions
Penning ionization in the sheath is very important
C Lazzaroni, P Chabert, M A Lieberman, A J Lichtenberg and A Leblanc, Plasma Sources Sci. Technol., 21, 035013 (2012)
C Lazzaroni, M A Lieberman, A J Lichtenberg and P Chabert J. Phys. D : Appl. Phys. 45, (2012) 495204
E Kawamura, M A Lieberman, A J Lichtenberg, P Chabert and C Lazzaroni
Plasma Sources Sci. Technol. 23 (2014) 035014
Plasma bulk
Electrode
Electrode
He/O2
~
1 mm
V. Schulz-von der Gathen et al., J. Phys. D 41 (2008) 194004
J. Waskoenig, Thesis, Queen’s University Belfast (2010)
J. Waskoenig et al. PSST 19 (2010) 045018

## Slide 37: Conclusions
Capacitive discharges are essential for plasma processing
After decades of research, there are still a lot of unknown phenomenon
Multi-frequency excitation is needed to control (almost) independently the ion flux and the ion energy to the wafer
However, it increases the complexity and the non-linear response of RF sheaths and the higher frequencies lead to non-uniformity
Higher pressure regimes are subject to mode transitions and related instabilities
Atmospheric pressure operation is possible but in small gap devices

## Slide 38: To learn more..
Principles of Plasma Discharges and Materials Processing,
M.A. Lieberman and A.J. Lichtenberg,
2nd Edition, John Wiley and Sons Inc., New York, 2005
Physics of Radiofrequency Plasmas
P. Chabert and N. Braithwaite,
Cambridge University Press, 2011
Foundations of capacitive and inductive radio-frequency (RF) discharges,
P. Chabert, T. Tsankov and U. Czarnetzki
Plasma Sources Science and Technology, 30 (2021) 024001