## Slide 1: Procédés plasmas de microélectronique sur substrats refroidis à des températures cryogéniques
T. Tillocher1, J. Nos1, R. Ettouri1, P. Lefaucheux1, R. Dussart1,
1 GREMI, Université d’Orléans, CNRS, Orléans, France

## Slide 2: Outline
1) Introduction : Basics of plasma etching
2) Deep cryoetching of silicon
3) Cryogenic etching processes

## Slide 3: 1) Introduction: Basics of plasma etching
Plasma etching consists in using a plasma to transfer a mask pattern in a layer or the substrate itself
=> physico-chemical interaction between the plasma and the substrate
Quick definition
Masked wafer
Mask
Layer
Substrate
Radicals
Mask
Cross section view
Chang & Cchen

## Slide 4: 1) Introduction: Basics of plasma etching
Plasma reactors
- Low pressure plasma reactors : mostly RF plasma etching tools (ICP, CCP), see P. Chabert’s talk
- Example below : industrial ICP etching reactor with loadlock (13.56 MHz RF frequencies)

## Slide 5: 1) Introduction: Basics of plasma etching
Basic etching mechanisms in low pressure plasmas
- Plasmas of reactive gases (mostly halogen-containing molecules)
- Both radicals and ions produced in the plasma are involved in the etch process
- Chemical etching (spontaneous):
Adsorption, chemical reaction between radicals and the surface and desorption of etch product
- Physical etching:
Ion bombardment at the surface
Ion induced etching, sputtering
- In an etch process, these 2 mechanisms happen at the same time… and more…

## Slide 6: 1) Introduction: Basics of plasma etching
Fields of application (very general)
Microelectronics
Optoelectronics
Microsystems – MEMS
https://www.photonics.com
https://www.extremetech.com
https://www.memsjournal.com
Main features of plasma etching : anisotropy, downscaling

## Slide 7: 1) Introduction: Basics of plasma etching
Cryogenic etching
Plasma etching with substrate temperature < -90°C
=> Use of liquid nitrogen
=> Specific design of the substrate holder (-150°C => 30°C)
First question: Can we etch at such low temperature?
=> YES, if the etch product is still volatile
=> Case of silicon compounds etched with F-based plasmas
Second question: Why etching at such low temperatures?
=> Etching of high aspect ratio profiles (deep silicon etching)
=> Specific behavior at cryogenic temperature (passivation, increased surface residence time)
=> Low damage etching and significantly reduced contamination of reactor walls

## Slide 8
Principle of the standard cryogenic process
O
ions
F
S
Fx
Si
F
4
SiO2 mask
Silicon (100) cooled down at -100°C and negatively biased
Passivation layer (SiOxFy)
Monocyclic SF6/O2 plasma
Chemical etching (selective)
SiF4 : main etch product
Simultaneous mechanisms
 Passivation layer (SiOxFy)
 Forms only at very low temperature
 Fragile passivation layer, easily removed by ion bombardment
2) Deep cryoetching of silicon
Etching of high aspect ratio features
=> Depth >> Critical Dimension (CD)

## Slide 9
2) Deep cryoetching of silicon
Low temperature + oxygen + bias = anisotropic structures
SF6 without bias
+30°C
-80°C
-50°C
-110°C
Anisotropic etching at -110°C, with oxygen
and bias
Passivation layer
formation on the sidewalls
+30°C
-50°C
-80°C
-110°C
SF6 /O2 without bias
+30°C
-50°C
-110°C
-80°C
SF6 /O2 with bias
20 µm
20 µm
20 µm
20 µm
20 µm
20 µm
20 µm
20 µm
20 µm
20 µm
Isotropic profile for all temperatures between +30 and -110°C
With oxygen, the profile is changed at very low temperature
Lozenge shape due to crystallographic effect at -110°C
20 µm
20 µm
20 µm
20 µm
20 µm

## Slide 10
Performances of the cryogenic process
2) Deep cryoetching of silicon
Example of profiles :
Holes (TSV)
CD = 14 µm
30 minutes
Advantages
Monocyclic process
 High etch rates, smooth sidewalls
Desorption of the passivation layer at room temperature  clean process
Depth = 210 µm
AR = 15
ER (30’) = 7 µm/min
Drawbacks
Very sensitive to temperature and O2 flow variations
Requires liquid nitrogen
ARDE is quite pronounced
100 µm
Positive slope
T°C 
Negative slope
T°C 
100 µm

## Slide 11
Applications
2) Deep cryoetching of silicon
Deep Etching is intensively in MEMS and microlectronic industries
Deep Trench Insulation
TSV for interconnects
3D capacitors
MOEMS
MEMS
50 µm
200 µm
200 µm
20 µm
20 µm

## Slide 12
Passivation mechanism
- SF6/O2 plasma interacting with a cooled silicon wafer
- The passivation layer is composed of silicon, oxygen and fluorine (~SiOF3, shown by XPS analyses)
 It is formed at the surface from SiFx and O species at the surface (not in gas phase)
 The passivation layer is more fluorinated as the temperature decreases
 The physisorbed layer desorbs at room temperature, which releases SiF4 (desorption mass spectrometry)
SiO2 mask
70 µm
400 µm
Etched part
Bulk Si
B
A
C
- The passivation layer is almost entirely removed when the substrate is warmed back up to room temperature
Ex-situ XPS
R. Dussart et al J. Micromech. Microeng., 14, 190-196 (2004)
2) Deep cryoetching of silicon

## Slide 13
Passivation mechanism
- A SiF4/O2 plasma can be used to grow a SiOxFy passivation layer on flat surfaces
 monitoring of growth by in-situ ellipsometry for different substrate temperatures
- During venting/warming of the sample, a part of the layer desorbs.
- Below -100°C, the deposited layer thickness decreases
G. Antoun et al. JJAP, 58, SEEB03 (2019)
O2 flow = SiF4 flow = 50 sccm
Psource = 1000 W
Pbias = 0 W
Pressure = 3 Pa
Process duration: 30 s
- Thicker layer by decreasing the temperature from 20 to -100°C
2) Deep cryoetching of silicon

## Slide 14
Passivation mechanism
30 s
O2
1000 W
30 s
SiF4
1000 W
10 s
Ar purge
w/o plasma
- Both SiFx species and O atoms are required to form the SiOxFy layer
- Decomposition of their role…
- Growth during the SiF4 plasma
- Thicker SiOxFy layer at low temperature
    Physisorption and accumulation of SiFx at the surface favored at low temperature
    Higher surface residence time
    Oxidation of the SiFx during the oxygen plasma (not detected by ellipsometry)
- Alternation of O2 plasma and SiF4 plasma
R. Dussart et al., J. Phys. D: Appl. Phys. 47 123001 (2014)
2) Deep cryoetching of silicon

## Slide 15: 2) Deep cryoetching of silicon
Passivation mechanism
Surface analysis
4 gas feed
Plasma
source
T controller
Sample rod
-180°C < T < +1100°C
Load lock
Differential pumping
Electron multiplier
Hemispherical analyzer
X-ray source
Electrostatic lenses
OPTIMIST Platform (IMN, Nantes) => Quasi in-situ XPS

## Slide 16
Passivation mechanism : in-situ XPS analyses
a-Si sample ; 30 s ; SiF4 /O2 : 25 % ; 3.0 Pa ; 200 W ICP power ; no bias
- SiOxFy layer growth at 3 different temperatures : -40, -65 and -100°C
- At -40°C, 17.1% [F] ; 23.6% [O]
=> After heating: no significant change
- At -65°C, 20.0% [F] ; 22.8% [O]
=> After heating: a little decrease of [F]
- At -100°C, 52.3% [F] ; 18.0% [O] ; 15% [N] (stoechiometry of ~SiOF3)
After heating: a large part of F-based species has desorbed (~SiO2)
G. Antoun et al 2022 ECS J. Solid State Sci. Technol. 11 013013
Optical index n of the order of 1.2 , which indicates that the remaining layer is quite porous
2) Deep cryoetching of silicon

## Slide 17
- SiF4/O2 plasma can reinforce the passivation layer => Time-multiplexed cryoetching
- Enhanced physisorption at cryogenic temperature
  => Low-damage cryogenic etching of low-k materials (not presented)
  => Cryogenic Atomic Layer Etching
Passivation mechanism: summary
2) Deep cryoetching of silicon

## Slide 18
0°C
Same experiment at
–83°C
Alternated cryogenic process
SF6 plasma step
SiF4/O2 passivation step
A few seconds to a few 10s µs for each step
 Anisotropic profiles
Role of substrate temperature
 4 alternances 1min SF6 etching - SiF4/O2 deposition + a final 1 min etch
Anisotropic microstructures can be eched provided the substrate is cooled at cryogenic temperature
T. Tillocher et al., J. Electrochem. Soc., Vol. 155, 3, D187-D191 (2008)
STiGer process
3) Cryogenic processes

## Slide 19: 3) Cryogenic plasma processes
Process based on capillary condensation of a high boiling point organic (HBPO) at low temperature
 Cooling at -50°C
 Pore Condensation of HBPO (flow of SF6/HBPO, 3 Pa)
SF6 or SF6/HBPO plasma (500W, 3 Pa, 1 min)
Annealing at 400°C under N2 (10 min)
Heating/Unloading
- Densified material is etched with strongly reduced diffusion of radicals and anisotropic profiles
- The k-value is very close to its initial value after process at -50°C
 Almost no PID at -50°C
Cryoetching of low-k materials
50°C
50°C
50°C
- Porous Organosilicate Glasses (p-SiOCH) are low-k materials used for advanced interconnects
 Very sensitive to plasma species (decrease of k-value)
Reduction of PID by cryogenic etching

## Slide 20: 3) Cryogenic plasma processes
Cooled
susbtrate holder
SiO2 substrate
Purge
Pumping
Adsorbed
layer
Ar plasma
Self-Limiting Etching
Precursor
w/o plasma
Purge
Etching
C4F8
Ar
Plasma
(ICP + bias)
C4F8
Ar Plasma
Ar gas
Pumping
Physisorption
0
0
0
Time
Cryogenic Atomic Layer Etching (CryoALE) of SiO2
Why Atomic Layer Etching (ALE) ?
- Atomic precision (scale reduction of Integrated Circuits)
- Etching of thin layers with no damage to underlying layers
- « Infinite » selectivity
Why CryoALE of SiO2 ?
- Prevent process drift due to reactor wall contamination

## Slide 21: 3) Cryogenic plasma processes
Adsorption
  C4F8 gas flow
  10 s
Purge
  Ar gas flow
  30 s
Etching
  Ar plasma
  2 min
  Source: 400 W
  Bias: -20 V
Pumping
  w/o gas
  15 s
- Self-Limiting Etch was reached
- Regular EPC 0.4 nm/cycle over 70 cycles
C4F8
Purge
Etching
SLE
G.Antoun et al, Appl. Phys. Lett. 115, 153109 (2019)
- No etching at -110 °C (and higher temperatures)
8 cycles
Cryogenic Atomic Layer Etching (CryoALE) of SiO2
- No drift, no wall contamination

## Slide 22: To summarize…
The authors would like to thank
for their valuable financial and scientific supports
Thank you !
This research was supported by CERTeM 5.0 platform, which provides most of the equipment, and funded by the European Union under project no EX004028. Europe is committed to the Centre-Val de Loire region with the European regional development fund
Benefit of cryogenic cooling of substrates for plasma etching
 Increased surface residence time of species => passivation, capillary condensation, physisorption…
 Less plasma induced damage
 Less contamination of chamber walls (layers deposited only on cooled surfaces)
Renewed interest of cryogenic industries in the industry… but little communication
 Alternative designs of cooling technologies (without liquid Nitrogen)
 Main argument = less damaging (lower radical diffusion)
 example: Flash Memories (vias in 3D NAND)