## Slide 1: Disentangling lattice and electronic instabilities in the excitonic insulator candidate Ta2NiSe5 by non-equilibrium spectroscopy
Yann Gallais
Katsumi et al. Phys. Rev. Lett. 130, 106904 (2023)

## Slide 2: Main players
Tr-Raman
Sample growth and characterization
Kota Katsumi
Alexandr Alekhin
Amir Haghighirad
Matthieu Le Tacon
S. Houver, M. Cazayous, A. Sacuto
M. Merz, S. Souliou

## Slide 3: Excitonic insulator: the concept
BCS
BEC
N. Mott Phil. Mag. ‘1961
D. Jérôme, T.M. Rice and W. Kohn, Phys. Rev. ‘1967

## Slide 4: TNS: an excitonic insultator ?
transport
optics
Ta2NiSe5
2D material
Small (zero?) direct band-gap at high-temperature
Semi-metal to insultator transition at 326K
Larkin et al. Nat. Comm. ‘2017

## Slide 5: TNS: an excitonic insultator ?
transport
optics
Ta2NiSe5
2D material
Small (zero?) direct band-gap at high-temperature
Semi-metal to insultator transition at 326K
ARPES experiments on TNS
Seki et al. Phys. Rev. B ‘2014

## Slide 6: Structural transition
Simultaneous structural transition
Is the insulating state a result of lattice distortion transition ?
Subedi et al. Phys. Rev. Mat. ‘2020
Watson et al. Phys. Rev. Res. ‘2020
Finite hybrization: gap opening and monoclinic distortion
Ortho. Phase: interchain Ni-Ta hopping is forbidden by mirror symmetry
DFT calculations
Non-equillibrium approach

## Slide 7: Time-resolved Raman scattering set-up
Raman : probe optical phonon and electronic excitations
Light polarizations: lattice symmetry
Stokes/anti-Stokes: excited state populations
Raman shift wi-ws:
energy of excitation
wi
ws

## Slide 8
spectrometer
Cryostat (3-300K)
Time-resolved Raman scattering set-up
Recent upgrade: pulse compressor (50 fs pulses)
2-color set-up

## Slide 9: Static Raman scattering: phonon
Mode 2: « monoclinic » B2g optical phonon
Raman selection rules: activated in aa geometry in monoclinic phase
Polarization dependence: marker of lattice distorsion
1

## Slide 10: Optical emission in the insulating phase
Opening of gap: quench of non-radiative processes
Increase of emission across the gap
Look for fingerprint of insulating gap at high Raman shift
Not Raman but Photoluminescence (PL) process !

## Slide 11: Out of equilibrium lattice dynamics
Lattice distortion is weakened in the first 4 ps but recovers afterwards
Remains in the monoclinic phase at all times
Time resolution: 2.5 ps
Energy resolution: 9 cm-1
Polarization resolved measurements
5
3
2
2

## Slide 12: Metastable gapless state
After 4 ps: optical emission is quenched to above Tc-like spectrum
Gapless metastable state with monoclinic structure
Favors excitonic scenario
Time resolution: 0.7 ps
Energy resolution: 3 cm-1

## Slide 13: Phonon Mode effective temperature
Effective phonon temperature:
Phonon Raman response:
Preferential coupling of photo-induced carriers to mode 2 phonon
Back to quasi-equilibrium after 15ps
Gapless state: not a thermal state (i.e. simple heating)

## Slide 14: Summary
Metastable gapless state….
….with preserved monoclinic distortion
An example of light induced metastable state with unique properties
Katsumi et al. Phys. Rev. Lett. 130, 106904 (2023)

## Slide 15: Origin of metastable state ?
Metastable red-shift of mode 5 optical phonon
Mode 5 is symmetry preserving: not related to monoclinic distortion
Not a simple heating effect
Possible metastable change of the lattice

## Slide 16: Raman spectra in equilibrium with CW laser
Above Tc
Tc = 326 K
Mode 2 in ac shows assymetric broadening
→ Fano lineshape due to the strong electron-phonon coupling
K. Kim et al., Nat. Comunn. 12, 1969 (2021)
P. A. Volkov, et al., npj Quantum Mater. 6, 52 (2021) from G. Blumberg Gr. [P2]
Black: Ag, Magenta: B2g defined above Tc
Mode 2 (70 cm-1) appears in aa below Tc

## Slide 17: Raman spectra in equilibrium with CW laser
Mode 2: Reporter of the structural symmetry breaking
Tc = 326 K
 | aa | ac
Above Tc | Ag | B2g
Below Tc | Ag | 
Raman selection rule
Above Tc

## Slide 18: Raman spectroscopy in equilibrium
 | aa | ac
Above Tc | Ag | B2g
Below Tc | Ag | 
Raman selection rule
CW laser
(514.5 nm)
aa : ei // a, eo // a
ac : ei // a, eo // c
Definition
Raman tensor below Tc
No separation
Raman tensors in ac-plane above Tc
Raman intensity

## Slide 19: Pump-probe Raman spectrosopy: Results
5
3
2
2
Pump fluence 1.7 mJ/cm2
Mode 2 and 3 intensities increases, while mode 5 intensity decreases.
Mode 2 in aa is finite after photoexcitation!

## Slide 20: Pump-probe Raman spectrosopy: Results
Mode-2 ratio decreases after pump: weakening monoclinic distortion
Note: time-resolution is 2.5 ps
After 5 ps, it is always greater than that above Tc
Structural symmetry remains in low-T monoclinic phase after photoexcitation
Mode-2 intensity ratio
Up to 2.8 mJ/cm2
1.7 mJ/cm2

## Slide 21: Phonon Mode effective temperature
Stokes
Anti-Stokes
Effective phonon temperature:
Phonon Raman response:
Preferential coupling of photo-induced carriers to mode 2 phonon
Back to quasi-equilibrium after 15ps
Gapless state: not a thermal state (i.e. simple heating)

## Slide 22: Pump probe reflectivity

## Slide 23: Out of equilibrium spectroscopy
principle
implementation

## Slide 24: Discussion : Metastable state with reduced PL
PL
Long-lived photoexcited carrier
→ Screen the Coulomb interaction
Temperature recovers to below Tc
→ Not the temperature increase
Phonon temperatures

## Slide 25: Electronic or structural instability ?
Lattice distortion -> finite hybridization -> gap opening
Excitonic instability -> finite hybridization -> lattice distortion
U-V Hartree Fock calculations: finite « excitonic » OP region
DFT: unstable optical phonon mode in ortho phase
Mazza et al. Phys. Rev. Lett. ‘2020
Sudebi, Phys. Rev. Mat. ‘2020
Windgatter et al. npj Comput. Mater. ‘2022
Ta
Ni
Out-of-equilibrium approach: decouples fast electronic from slow lattice degrees of freedom