## Slide 1: Sustainability Workshop 2023 Nov. 16. – Nov. 17. 2023 Reuse of Tunnel Excavation Material WP 9
Elisabeth Hauzinger – Montanuniversität Leoben (Austria)

## Slide 2: Why Reuse of Tunnel Excavation Material?
500 million tons construction & demolition waste in EU per year, only 25% are recycled.
© Eurostat
Scarcity of Building Raw Materials
Longer transport routes
Higher CO2 emissions
Import dependency
Average composition of excavated tunnel material from hard and soft rock tunnel construction projects
© DRAGON
© Kündig et al., 1997

## Slide 3: General Conditions
Technical
Geological
Chemistry/ mineralogy/ strength properties of excavated materials
Legal
Tunnel advance method, -length, -diameter
Material yield parameters
Customer specifications
Economic
Supply and demand
Material analysis
Processing technology
End of waste character
Ownership
Transport route/ -range to customers / landfills
Site organisation
Processability
Raw material price vs. landfilling costs
Geological situation
Waste law

## Slide 4: Geological Investigations
Geotechnical
UCS, Tensile Strength, CERCHAR Test Point Load, LCPC Test, …
Geochemical & Petrophysical
Eluate, water absorption, porosity & permeability, density, TOC, …
Mineralogical
XRD, XRF, ICP-MS, Optical Microscopy, FTIR, …
(Borehole-) Geophysics
Gamma-Gamma, SP, Dilatometer, Seismics, …
Classification of Subsurface |  | 
Rock classification | Mineral composition | Rock descriptions
Very weak marl | - | Numerous, closed micro-fissures, low stiffness, ductile behaviour, swelling potential
Weak marl | Clay=45-60, quartz=15-30, calcareous minerals=20-30 | Micro-crystalline quartz, medium-high plasticity, minor micro-fissures, swelling potential
Medium-weak marl | Clay=20-45, quartz=20-40, calcite=20-30 | Well cemented, low plasticity
Weak sandstone | Clay=5-20, quartz=40-70, calcareous minerals=5-45, feldspar=5-10 | Fine-grained, poorly cemented
Medium sandstone |  | Rare discontinuities
Strong sandstone |  | Better cemented, fewer discontinuities
Investigations of the Underground
Wide ranged investigation methods
Results
Geological characterisation
Einstein Telescope
Triangular or L-shape, total tunnel length of 30 km & diameter of 7 m
Together with caverns, service & access tunnels and shafts  total excavated volume ~ 4.4 Mio m3 ↔ muck volume ~ 5.3 m3
Exact location not yet determined
© ET Symposium April 2018
© Haas (2022)

## Slide 5: Strategies for Reuse of Tunnel Excavation Material
Graphic representation of underlying forecast reliability and associated recovery and landfill classes of a tunneling project in phase A of the main investigations (ÖBV 2015)
Strategies for reuse
Strategies for the reuse of excavated material should at least meet following requirements:
Technical Feasibility
Economic Viability
Social Benefits
Project Relevance
Real time characterisation of material
Onsite online-analyses on conveyors to detect impurities and pollutions as well as grain size
Sorted and classified material is processed further into respective products
© Terzis et al. (2021)
© CERN 2022

## Slide 6: Reuse Scenarios
Recycled construction materials
Substitute for secondary construction materials
Industrial raw materials
Geotechnical Parameters
Aggregates for concrete & shotcrete
Road construction
Railway ballast
…
Mineralogical & chemical parameters
Low Carbon Cement
Geopolymers
Raw Earth Bricks
Mineral Wool
…
Silica Sands
Magnesite
Feldspar
Mica
Sulfates
Clay minerals
…
Voroin et al. (2021)
Graftieaux et al. (2021)
© Carlesso et al. (2021)